Epitaxial n++-InGaAs ultra-shallow junctions for highly scaled n-MOS devices

P. Tejedor,1,a) M. Drescher,2b), L. Vázquez,1 and L. Wilde2c)

1Instituto de Ciencia de Materiales de Madrid, C.S.I.C.. Sor Juana Inés de la Cruz 3, 28049 Madrid, Spain

2Fraunhofer IPMS-CNT, Königsbrückerstraße 178, 01099 Dresden, Germany

a) Author to whom correspondence should be addressed.  E-mail:  ptejedor@icmm.csic.es

b)Present address: GlobalFoundries. Wilschdorfer Landstr. 101, 01109 Dresden, Germany

c)Present address: Ernst-Abbe-Hochschule Jena. University of Applied Sciences. Carl-Zeiss-Promenade 2, 07745 Jena, Germany

Declarations of interest: none

Abstract

High electron mobility III-V semiconductors like InGaAs are excellent candidates for sub-10 nm n-metal-oxide-semiconductor (nMOS) devices. One of the critical challenges in downscaling III-V devices is achieving low-resistance contacts by forming low-defect, ultra-shallow junctions less than 9 nm in depth, with n-type dopant concentrations above 1019 cm-3. In the current study, we combine time-of-flight secondary ion mass spectrometry (ToF-SIMS) depth profile analysis, atomic force microscopy (AFM) imaging, and high-resolution transmission electron microscopy (HR-TEM) to determine the optimal doping strategy for growing Si-doped n++-In0.25Ga0.75As ultra-shallow junctions by molecular beam epitaxy. We test three different approaches to doping: homogeneous co-deposition, single δ-layer (continuous) doping, and triple δ-layer (pulsed) doping. We demonstrate the formation of technologically suitable n++-In0.25Ga0.75As junctions 5-7 nm deep, grown under As-rich conditions with a single δ-layer at temperatures as low as 400ºC. These junctions have peak Si concentrations between 6x1019 and 1x1020 cm-3 and high crystal quality. The surface self-organizes into smooth ripples or mounds, up to a peak dopant concentration of ~2x1020 cm-3. Above this value, enhanced diffusion of Si and In due to a large population of Ga vacancies increases lattice strain in the semiconductor epilayer, triggering a transition from 2D growth to 3D growth and the formation of In0.85Ga0.15As clusters on the surface.

KEYWORDS:  indium gallium arsenide, ultra-shallow junctions, semiconductor growth, time-of-flight secondary ion mass spectrometry, solid-state diffusion, self-organization.

- Introduction

Replacing the strained Si channel with high electron mobility III-V compound semiconductors, particularly InGaAs, is considered one of the best ways to improve the drive current in sub-10 nm metal-oxide-semiconductor field-effect-transistors (MOSFETs) at low supply voltages [1,2]. As devices decrease in size, the scaling of the source/drain contact geometries results in current crowding and increased access resistance. Mitigating this effect is one of the most difficult challenges in the fabrication of highly scaled III-V MOSFETs [3-6]. In this respect, heavy doping of the source/drain (S/D) regions to form an abrupt, ultra-shallow, and damage-free junction is essential to suppress the source-to-drain leakage current and other short channel effects. However, traditional Si+ ion implantation of InGaAs at high doses induces amorphization and stacking faults. The resulting surface requires thermal annealing above 550ºC to repair the ion-induced crystal damage and activate dopants. Despite recent progress in mitigating this damage through elevated implant temperatures, the technique still results in broad dopant distributions and low levels of electrically active dopants. So far, these disadvantages have prevented Si+ ion implantation from being used to fabricate nanoscale ultra-shallow junctions (USJs) [7-9]. Conformal monolayer doping offers great prospects for the fabrication of three-dimensional logic devices such as fin-FETs and nanowire-FETs, and has been demonstrated for Si-doped GaAs and InGaAs [10-12]. Its main drawback is the need for a dielectric capping layer, which prevents the dopant from desorbing from the surface during laser annealing or rapid thermal annealing. Annealing induces diffusion into the semiconductor and activates the dopant. In contrast with the two methods just mentioned, molecular beam epitaxy (MBE) allows the deposition of highly doped III-V ultra-shallow junctions (USJs) in a single step at relatively low temperatures, while providing the strict control over layer thickness, doping concentration, and dopant spatial distribution required in ultra-small scale devices [13-15].

A recent review by Aldridge et al.[16] addresses the main challenges to minimizing contact resistance and achieving the highest possible level of activation for n-type InGaAs doped with Si using the aforementioned techniques (i.e., ion implantation, monolayer doping, and molecular beam epitaxy). They point out that the limits to n-type dopant activation in InGaAs are mediated by compensating point defects, whose formation is closely related to the concentration-dependent Si diffusion observed in heavily n-type doped InGaAs regions. Despite this obstacle, low-temperature epitaxial doping methods are currently considered the most promising approach to maximize the activation of n-type dopants. Therefore, there is an urgent need for methods to overcome dopant-vacancy complexing in this context.

In this article, we present a comparative study of nanoscale, Si-doped, n++-InGaAs ultra-shallow junctions with depths ≤9 nm, grown on GaAs(001) substrates by MBE using three methodologies: homogeneous dopant co-deposition (volume doping), single δ-layer doping, and pulsed δ-layer doping. We study the junctions using time-of-flight secondary ion mass spectrometry (ToF-SIMS) to measure ion depth profiles, atomic force microscopy (AFM) imaging, and high-resolution transmission electron microscopy (HR-TEM). The goal of this research is to investigate the effect of the local dopant concentration on the structure of the junction, the stability of the InGaAs growth front, and surface self-organization during deposition of the first 10-20 ML, i.e., 5-9 nm. We also wish to study relationships between these properties and other relevant atomic processes, such as Si and In diffusion. We demonstrate the formation of abrupt, single δ-layer doped, n++- In0.25Ga0.75As junctions 5 nm in depth, with Si concentrations close to 9x1019 cm-3 and atomically smooth surface morphologies. These junctions possess properties suitable for sub-10 nm device fabrication. We also show that degradation of the nanoscale surface morphology is linked to the formation of point defects and the onset of a growth mode transition from 2D to 3D. The degradation begins to occur for Si concentrations above ~2×1020 cm-3, an order of magnitude higher than the previously reported limit for thicker n++-InGaAs junctions.

- Material and Methods

All Si-doped In0.25Ga0.75As samples (hereafter referred to as InGaAs) were grown in a solid-source RIBER Compact-12 III-V MBE system equipped with a 10 keV electron gun for reflection high-energy electron diffraction (RHEED) measurements. Elemental Ga and In were supplied by conventional effusion cells, while As2 was provided by a Mark-V (Veeco) cracker cell. The Ga, In and As2 fluxes were calibrated using the RHEED intensity oscillation technique on a GaAs (001) substrate with the aid of a kSA-400 RHEED analysis system. Si doping was carried out using a conventional effusion cell heated to 1100-1200ºC. The GaAs (001) substrates (Wafer Technology Ltd.) were outgassed at 350ºC then heated to 610ºC to remove the native surface oxide, under an As2 flux of ~1x1015 molecules cm-2 s-1. A 100 nm thick GaAs buffer layer was then deposited, followed by the growth of 5-8 nm thick n++-InGaAs layers at temperatures between 375ºC and 430ºC, with a constant V/III flux ratio of 40:1 at a rate of 0.4 μm/h. The deployment of high As overpressures during growth of the n-type InGaAs epilayers was intended to induce preferential Si incorporation to cation sites and lower the anion vacancy concentration. Three different techniques were used in this study to dope the InGaAs epilayers with Si, as shown in Figure 1: (i) volume doping by co-deposition during growth; (ii) single-δ doping for 20s to 60s after InGaAs growth interruption, followed by resumption of growth; and (iii) triple-δ doping with identical Si pulses having 20s to 60s duration, separated by 2 nm thick In0.25Ga0.75As layers.

Elemental depth profiles of the n++-InGaAs samples were acquired in dual-beam mode, using a time-of-flight secondary ion mass spectrometer equipped with two ion sources (ToF.SIMS 300R, ION-TOF GmbH). A liquid metal ion gun (LMIG) was used to generate clusters of 25 keV Bi+ ions for the analysis beam, and an electron impact gun was used to generate 0.5 keV Cs+ ions for the sputtering beam. In this mode, the Bi+ beam was rastered over a 102 ×102 μm2 area and centered inside the 400×400 μm2 Cs+ crater. Target currents were measured separately before each depth profile using a Faraday cup. The Bi+ current was 0.8 pA and the Cs+ current was 29.5 nA. A low-energy electron flood gun was used for charge compensation throughout all depth profiles. A In0.53Ga0.47As:Si doped sample with a uniform Si concentration of 2x1018cm-3, previously calibrated by electrochemical capacitance-voltage profiling, was used as a reference to calculate the Si concentration in the In0.25Ga0.75As USJs grown by MBE. The sputter time was 300s for all samples except the reference specimen, for which it was 500s. Sputtering yields were determined by dividing the total sputtered volume (using the size of the rastered area and the thickness measured by cross-sectional transmission electron microscopy) by the total primary ion fluence used during the sputtering time. The sputtering yield was assumed to remain constant during the depth profiling experiments.

The surface morphology of the Si-doped InGaAs samples was examined with a 5500 Agilent AFM microscope (Agilent Technologies, USA) operating in dynamic mode under ambient conditions. Images consisting of 1024x1024 pixels were recorded with Si cantilevers (Bruker Corp., UK) having a nominal spring constant of 40 N/m and a nominal end radius of 8 nm. Cross-sectional specimens suitable for HR-TEM were prepared using a focused ion beam (FIB) FEI Strata 400 STEM dual-beam system. The specimens were examined in a Philips Tecnai F20 TEM/STEM operating at 200 keV and equipped with an integrated system for energy dispersive spectroscopy (EDS) analysis. Bright field TEM images were recorded.

- Results and discussion

We used AFM to examine the surface morphology of the volume-doped Si:InGaAs samples as a function of two experimental parameters: growth temperature and Si effusion cell temperature (the latter is directly related to Si atomic flux). Between 375ºC and 430ºC, growth proceeds through the nucleation of two-dimensional (2D) islands in the presence of Ehrlich-Schwoebel barriers to adatom diffusion across step edges, as shown in the 1x1 μm2 images gathered in Figure 2. The root mean square (rms) roughness increases slightly with both parameters between 0.24 and 0.54 nm, as indicated in the images.

Figure 3 presents ToF-SIMS depth profiles of the volume-doped InGaAs USJs, to demonstrate the effect of Si cell temperature and substrate temperature on the peak Si concentration and the shape of the Si distribution. Under the experimental conditions here studied, peak Si concentrations between 1.4x1019 and 1.2x1020 cm-3 were attained in volume-doped samples. Results showed that reaching doping levels in the 1020 cm-3 range required the deployment of Si cell temperatures as high as 1200ºC, since the peak Si concentration increases with the Si atomic flux. It was also found that, for a constant Si flux, the incorporation of Si in the InGaAs lattice increases with decreasing substrate temperatures. But it is worth noting that, while the peak Si concentration increases only slightly, the junction depth undergoes a more pronounced change at lower temperatures: Taking as a reference a doping level of 1x1018 cm-3 the measured junction depth in the sample grown at 375ºC is approximately 2 nm wider than those in samples grown at temperatures of 400ºC or higher. In addition, all depth profiles depicted in the graph exhibit a more or less pronounced shoulder, which points to the existence of concentration-dependent Si diffusion in volume-doped InGaAs layers within the doping level range examined, i.e., 1.4x1019 - 1.2x1020 cm-3. Although historically Si has been the preferred n-type dopant for group III arsenides due to its limited diffusivity upon thermal annealing, our results agree with recent diffusion studies carried out in 50 nm thick volume-doped Si:InGaAs samples, which have demonstrated that Si diffuses very rapidly in concentrations above 1-3x1019 cm-3, but is immobile below this range [14-16].

Based on the results described above, we chose to grow the single-layer and triple  -layer doped InGaAs USJs at a substrate temperature of 400ºC with a fixed Si cell temperature of 1200ºC. ToF-SIMS depth profiles of the Si concentration in δ-layer doped samples are gathered in Figure 4. Figure 4a depicts four concentration profiles, corresponding to single δ-layer doped InGaAs USJs prepared with 20, 30, 40 or 60s growth interruptions to deposit the δ-layer. The peak Si concentration values range from 6.5x1019 to 1.4x1020 cm-3. The distributions are symmetric and increase in width with dopant concentration, with full-width-at-half-maximum (FWHM) values between 1.3nm (20s δ-layer) and 1.5nm (60s δ-layer). It is worth noting that these widths are approximately half of that found for the volume-doped Si:InGaAs samples prepared with identical Si flux (Tcell=1200ºC) and substrate temperature  (FWHM=3.1 nm, see Figure 3). We also prepared three InGaAs USJs doped with three Si δ-layers deposited over 20s, 40s or 60s intervals (pulses). In the ToF-SIMS profiles of these samples, shown in Figure 4b, the peak Si concentrations increased with pulse length from 1.2x1020 to 3.0x1020 cm-3. The corresponding FWHM values ranged between 1.4 nm (3×20s δ-layers) and 1.8 nm (3×60s δ-layers). In comparison with the single δ-layer doped samples, triple δ-doped InGaAs junctions reached higher peak Si concentrations, but individual Si δ-layers cannot be resolved in the profiles, despite the 2 nm-thick InGaAs layer deposited between them. The samples exceeding concentrations of 2.4x1020 cm-3 (40s and 60s pulses) have slightly asymmetric dopant distributions. This is further evidence for enhanced diffusivity of Si in InGaAs above a critical Si concentration, which, according to our results, is 2.4x1020 cm-3 for δ-doped samples and one order of magnitude lower for volume-doped ones.

Arsenic and gallium ToF-SIMS depth profiles did not exhibit significant variations with respect to growth temperature or doping technique. In contrast, we did observe the accumulation of indium on the surface of both volume-doped and δ-layer doped InGaAs samples, as illustrated in Figures 5a-c. This effect is more pronounced at higher substrate temperatures, and results in the formation of ternary alloys in the first atomic layers. These alloys have a much higher In content than expected from the effect of segregation during growth at temperatures below 450ºC [17].  The surface composition calculated from the depth profiles is In0.45Ga0.55As in samples grown at 375ºC, but In0.85Ga0.15As in those prepared between 400º and 430ºC. It can also be observed in Figure 5c that the InGaAs samples doped with triple Si δ-layers of 40s and 60s duration exhibit broader indium profiles than the one doped with 20s δ-layers, which implies an enhancement of In diffusion in parallel with the enhanced Si diffusion at high Si concentrations. To better compare the three doping methodologies deployed, Figure 6 gathers the depth profiles and the corresponding 3D reconstructions of the final Si distributions in InGaAs samples grown at 400ºC, with peak dopant concentrations of approximately 1x1020 cm-3. The figure clearly shows that, for a given doping concentration, InGaAs:Si samples doped with a single δ-layer exhibit shallower junctions with optimal lateral abruptness. On the other hand, the reconstructed 3D In distributions do not show significant differences with doping methodology.

The large-scale surface morphologies of the single and triple δ-layer doped n++-InGaAs junctions grown at 400ºC were investigated by AFM as a function of Si concentration. The 10x10 µm2 images gathered in Figures 7a-d provide evidence for the formation of smooth ripples running along the [1-10] direction at the lowest Si concentrations. As the doping concentration increases, the ripple structure destabilizes [18,19], breaking down into a mound morphology that is fully developed at doping levels above ~1x1020cm-3 in both single and triple δ-doped junctions. Both the lateral periodicity of the ripples/mounds and the rms surface roughness increase with Si concentration, regardless of the doping method employed, which reflects a progressive increase of the step edge diffusion barriers. This effect is further illustrated in the phase diagram shown in Figure 8. When the doping level exceeds 2.4x1020 cm-3, a value only attained through the deposition of three Si δ-layers over growth interruptions of 40s or longer, we see a transition from 2D to 3D growth that results in the formation of irregular clusters on the surface. The average size of these clusters is approximately 80 nm, as shown in the insets of Figures 7e and 7f.

High-resolution TEM studies of single and triple δ-layer doped n++-InGaAs, gathered in Figure 9, showed good agreement with AFM results. Cross-sectional images of InGaAs USJs having Si concentrations up to 1.4x1020 cm-3 exhibited planar surfaces, with no structural defects in the InGaAs layers (a). USJs with Si concentrations of 2.4x1020 cm-3 or higher had rougher surfaces (b) as a result of the growth mode transition described above.  It is worth emphasizing that the critical Si concentration for surface morphology degradation in sub-10nm USJs is almost one order of magnitude higher than the value of 4x1019 cm-3 previously reported for micron deep junctions by Fedoryshyn [13].

It is well established that surface undulations (ripples) form during the early stages of growth in unintentionally doped In0.25Ga0.75As layers deposited on GaAs substrates. This formation is a mechanism to reduce lattice strain, thus contributing to plastic relaxation below the critical thickness for dislocation formation.20,21 According to this interpretation, it would be reasonable to expect similar lattice strain and hence surface morphology in the single and triple δ-layer series of n++-InGaAs samples, which were grown at the same temperature, with the same nominal composition, and with the same capping layer thickness. Therefore, the destabilization of surface ripples giving way to a mound morphology is most likely a direct consequence of the increasing dopant concentration, in good agreement with previous kinetic Monte Carlo (KMC) simulations [19].

Moreover, in a USJ with heavy n-type doping, theory predicts that the III-V semiconductor Fermi level is shifted towards the conducting band, creating a high concentration of point defects (in this case gallium vacancies).22-24 This is confirmed by experimental observations such as scanning tunneling microscopy and positron annihilation spectroscopy [25,26].  The nucleation of excess vacancies in both ion-implanted and low-temperature grown InGaAs has been reported to increase the InGaAs lattice parameter much more than would be expected by simple dopant substitution [27,28], and also to enhance the diffusivity of species that can diffuse through a group III-vacancy mechanism [16,29].

The above arguments suggest that the strong segregation of In towards the surface (see Figure 5) is partly a consequence of the superdilation-related InGaAs lattice strain generated by Ga vacancies. Our ToF-SIMS and AFM results clearly demonstrate the existence of a critical Si concentration at which the concentration of Ga vacancies is sufficiently high to enhance the effective diffusivity of both Si and In. Both elements are known to diffuse through a group III-vacancy mechanism [15, 30]. While single and triple δ-layers with Si peak concentrations up to 1.4x1020cm-3 yield abrupt and damage-free n++-InGaAs USJs suitable for sub-10 nm devices, exceeding a critical Si concentration of 2.4x1020cm-3 results in deeper InGaAs junctions with broadened Si (triple δ-layer) doped regions and degraded surface morphology induced by the strain relief in the In-rich upper InGaAs atomic layers. Specifically, the surface begins to form 3D islands, hindering the practical applicability of the USJs.

Conclusions

In summary, we have investigated the effects of three doping techniques: homogeneous Si co-deposition (volume doping), single δ-layer deposition, and pulsed triple δ-layer deposition on the dopant distribution with depth, crystal structure, and surface morphology of nanoscale n++-InGaAs junctions grown by MBE, particularly those suitable for applications as S/D extended regions in sub 10 nm nMOS devices. We have shown that single δ-layer doping is the best option to achieve maximum Si dopant concentrations with good lateral abruptness, crystal quality and surface morphology. Using this approach, we were able to create 5 nm-deep n++-InGaAs junctions with doping levels close to 9x1019cm-3, narrow Si distribution depth profiles (FWHM of 1.4 nm), smooth surfaces (rms roughness of 0.6 nm), and free of structural defects. Evidence of In surface segregation was found in all samples, regardless of doping method, a situation that can be circumvented in future experiments by increasing the V/III flux ratio or decreasing the growth rate. Si doping levels in excess of ~1.4x1019cm-3 in volume-doped InGaAs and above 2.4x1020cm-3 in triple- layer doped samples significantly enhance the Si and In diffusion associated with Ga vacancies. This concentration-dependent effect increases the FWHM of the Si δ-layer and the width of the USJ, and induces three-dimensional growth on the USJ surface.

Acknowledgments

This work was financially supported by Ministerio de Economía y Competitividad of Spain (Grant numbers TEC2016-78433, MAT2017-85089-C2-1-R), by CSIC (Grant number 201880E058). P.T. acknowledges support from CSIC Research Platform on Quantum Technologies PTI-001.

References

[1] J.A. del Alamo, Nanometre-Scale Electronics with III–V Compound Semiconductors, Nature  479, (2011) 317-323.

[2] Jacob, A.P., Xie, R,, Sung, M.G.; Liebmann, L., Lee, R.T.P., Taylor, B., 2017. Scaling challenges for advanced CMOS devices, International Journal of High Speed Electronics and Systems, 26, 1740001.

[3] Masudy-Panah, S., Wu, Y., Lei, D., Kumar, A., Yeo, Y.-C., Gong, X., 2018. Nanoscale metal-InGaAs contacts with ultra-low specific contact resistivity: Improved interfacial quality and extraction methodology. J. Appl. Phys. 123, 024508.

[4] R.T.P. Lee, W.Y. Loh, R. Tieckelmann, T. Orzali, C. Huffman, A. Vert, G. Huang, M. Kelman, Z. Karim, C. Hobbs, R.J.W. Hill, S.S.P. Rao, Technology options to reduce contact resistance in nanoscale III-V MOSFETs, ECS Trans. 66 (2015) 125-134.

- [5] Singisetti, U., Wistey, M.A., Zimmerman, J.D., Thibeault, B.J., Rodwell, M.J.W., Gossard, A.C., Bank, S.R., 2008. Ultralow resistance in situ ohmic contacts to InGaAs/InP, Appl. Phys. Lett. 93, 183502.

- [6] I. Thayne, S. Bentley, M. Holland, W. Jansen, X. Li, D. Macintyre, S. Thoms, B. Shin, J. Ahn, P. Macintyre, III-V nMOSFETs- Some issues associated with roadmap worthiness, Microelectron. Eng. 88 (2011) 1070-1075.

- [7] A. Veloso, A. De Keersgieter, P. Matagne, N. Horiguchi, N. Collaert, Advances on doping strategies for triple-gate finFETs and lateral gate-all-around nanowire FETs and their impact on device performance, Mater. Sci. Semicond. Process., 62 (2017) 2-12.

- [8] A.G. Lind, H.L. Aldridge, C.C. Bomberger, C. Hatem, J.M.O. Zide, K.S. Jones, Fermi-level effects of extended defect evolution in Si+ and P+ implanted In0.53Ga0.47As. ECS J. Solid State Sc. 5 (2016) 3073-3077.

[9] B. Wood, C. Hatem, X. Bao, H. Zhou, M. Zhang, M. Jin, H. Chen, M.-P. Cai, S.S. Munnangi, M. Okazaki, E. Sanchez, A. Brand, Improvement of Si doping of In0.53Ga0.47As fin by heated implant. VLSI Technology, Systems, and Applications 1 (2015) 63-64.

- [10] J.C. Ho, R. Yerushalmi, Z.A. Jacobson, Z. Fan, R.L. Alley, and A. Javey, Controlled nanoscale doping of semiconductors via molecular monolayers, Nat. Mater. 7 (2008) 62-67.

- [11] O’Connell, J., Biswas, S., Duffy, R., Holmes, J.D., 2016. Chemical approaches for doping nanodevice architectures. Nanotechnology, 27, 342002.

- [12] J. O’Connell, E. Napolitani, G. Impellizzeri, C. Glynn, G.P. McGlacken, C. O’Dwyer, R. Duffy, J.D. Holmes, Liquid-phase monolayer doping of InGaAs with Si-, S-, and Sn-containing organic molecular layers ACS Omega, 2 (2017) 1750-1759.

- [13] Y. Fedoryshyn, M. Beck, P. Kaspar, H. Jaeckel, Characterization of Si volume- and delta-doped InGaAs grown by molecular beam epitaxy. J. Appl. Phys. 107 (2010) 0937101-0937103.

- [14] H. Aldridge Jr, A.G. Lind, C.C. Bomberger, Y. Puzyrev, C. Hatem, R.M. Gwilliam, J.M.O. Zide, S.T. Pantelides, M.E. Law M.E., K.S. Jones, Implantation and diffusion of silicon marker layers in‎ In0.53Ga0.47As,  J. Electron. Mater. 45 (2016) 4282-4287.

- [15] A.K. Baraskar, M.A. Wistey, V. Jain, U. Singisetti, G. Burek, B.J. Thibeault, Y.J. Lee, A.C. Gossard, M.J.W. Rodwell, Ultralow resistance, nonalloyed ohmic contacts to n-InGaAs, J. Vac. Sci. Technol. B 27 (2009) 2036-2039.

- [16] H. Aldridge Jr, A.G. Lind, C.C. Bomberger, Y. Puzyrev, J.M.O. Zide, S.T. Pantelides, M.E. Law, K.S. Jones, N-type doping strategies for InGaAs, Mater. Sci. Semicond. Process. 62 (2017) 171-179.

- [17] S.Y. Karpov, Y.N. Makarova, Indium segregation kinetics in InGaAs ternary compounds, Thin Solid Films 380 (2000) 71-74.

- [18] P. Tejedor, P. Šmilauer, C. Roberts, B.A. Joyce, Surface morphology evolution during

- unstable homoepitaxial growth of GaAs(110), Phys. Rev. B, 59 (1999) 2341-2345.

- [19] R. Sathiyanarayanan, A.B.H. Hamouda, A. Pimpinelli, T.L. Einstein, Role of codeposited impurities during growth. II. Dependence of morphology on binding and barrier energies, Phys. Rev. B, 83, (2011) 0354241-0354246.

- [20] M. Albrecht, S. Christiansen, J. Michler, W. Dorsch, H.P. Strunk, P.O. Hansson, E. Bauser, Surface ripples, crosshatch pattern, and dislocation formation: Cooperating mechanisms in lattice mismatch relaxation, Appl. Phys. Lett. 67 (1995) 1232-1234.

- [21] N.S. Chokshi, J.M. Millunchick, Cooperation nucleation leading to ripple formation in InGaAs/GaAs films, Appl. Phys. Lett. 76 (2000) 2382-2384.

- [22] W. Walukiewicz, Defect formation and diffusion in heavily doped semiconductors, Phys. Rev. B 50 (1994) 5221-5225.

- [23] W. Walukiewicz, Intrinsic limitations to the doping of wide-gap semiconductors, Phys. B

- Condens. Matter. 302 (2001) 123-134.

- [24] H.-P. Komsa, A. Pasquarello, Intrinsic defects in GaAs and InGaAs through hybrid

- functional calculations, Physica B 407 (2012) 2833-2837.

### [25] J. Gebauer, R. Krause-Rehberg, C. Domke, Ph. Ebert, K. Urban, Identification and quantification of defects in highly Si-doped GaAs by positron annihilation and scanning tunneling microscopy, Phys. Rev. Lett. 78 (1997) 3334-3337.

- [26] J. Mahony, P. Mascher, Positron-annihilation study of vacancy defects in InAs, Phys. Rev.

- B 55 (1997) 9637-9641.

- [27] J.B. Mullin, B.W. Straughan, C.M.H. Driscoll, A.F.W. Willoughby, Lattice superdilation phenomena in doped GaAs, J. Appl. Phys. 47 (1976) 2584-2587.

- [28] L. Survase, M. Nyayate, S. Mathew, Growth and characterization of Si-doped

- InGaAs/GaAs single quantum well, IOSR J. Appl. Phys. 6 (2014) 47-50.

- [29] G. Jia, J. Yao, Y. Shu, X. Xing, B. Pi, Effect of indium distribution on optical properties in

- InGaAs/GaAs quantum wells, Front. Optoelectron. China, 2, (2009) 108-112.

- [30] M. Kulik, A.P. Kobzev, D. Jaworska, J. Żuk, J. Filiks, Investigation of Indium

- diffusion process in In+ ion implanted GaAs, Vacuum 81(2007) 1124-1128.

Graphical abstract

Figures

Figure 1. Schematic of (a) volume doped, (b) single Si δ-layer doped, and (c) triple Si δ-layer doped n++-In0.25Ga0.75As:Si. All layers are grown by MBE.

Figure 2.  AFM (1x1µm) images showing variations in the surface morphology of 5 nm-thick volume-doped n++-In0.25Ga0.75As: Si samples grown from molecular beams of As2, Ga, In and Si. The images represent five separate experiments performed at different substrate growth temperatures and Si effusion cell temperatures.

Figure 3. ToF-SIMS Si depth profiles in volume-doped n++-In0.25Ga0.75As:Si samples grown at different substrate temperatures and Si atomic fluxes (i.e., Si effusion cell temperatures).

Figure 4. ToF-SIMS depth profiles of Si in (a) single -layer doped and (b) triple -layer doped n++- In0.25Ga0.75As:Si shallow junctions (5-9 nm) grown on GaAs (001) substrates at a substrate temperature of 400ºC.

Figure 5. ToF-SIMS depth profiles of As, Ga and In corresponding to n++ -In0.25Ga0.75As USJs grown at 400ºC by (a) volume-doping to a Si concentration of NSi=1.5x1020cm-3, (b) single -layer doping over 20s, 40s or 60s intervals to Si concentrations of NSi=6.5x1019cm-3 to 1.4x1020cm-3, and (c) triple -layer doping over 20s, 40s or 60s intervals to Si concentrations of NSi=1.2x1020cm-3 to 3.0x1020cm-3.

Figure 6. Comparison of doping methodologies: ToF-SIMS Si concentration profiles (left) and ToF-SIMS images showing 3D spatial distributions (right) of Si and In in (a) volume-doped, (b) single d-layer doped and (c) triple d-layer doped n++-In0.25Ga0.75As:Si samples having approximately the same peak dopant concentration (NSi≈1x1020cm-3).

Figure 7. AFM (10 µm×10µm) images of surface morphology evolution with increasing Si concentration in n++ -In0.25Ga0.75As:Si USJs grown at 400ºC. Samples with a single Si -layer: (a) t=20s, NSi=6.5x1019cm-3, (b) t=40s, NSi=8.8x1019cm-3, (c) t=60s, NSi=1.4x1020cm-3. Samples with three Si -layers: (d) t=20s, NSi=1.2x1020cm-3, (e) t=40s, NSi=2.4x1020cm-3, and (f) t=60s,  NSi=3.0x1020cm-3. The 2D to 3D growth mode transition is evident at NSi=2.4x1020 cm-3 and higher concentrations.

Figure 8. Phase diagram of Si concentration vs. rms roughness for the n++ -In0.25Ga0.75As surface morphology of various samples, showing the progressive formation of ripples, mounds and three-dimensional clusters.

Figure 9.  High-resolution TEM cross-sections showing the effect of Si doping concentration on the n++-In0.25Ga0.75As surface structure: (a) Structure after single δ-layer doping for 40s to a peak concentration of NSi=8.8x1019cm-3, (b) Structure after triple δ-layer doping for 60s to a peak concentration of NSi=3.0x1020cm-3.